
Application:	Thanks to its low viscosity, Acrydur® 440 is suitable as an accelerator for MMA coating resins applied at low floor temperatures.

Characteristics:  Accelerator Acrydur® 440 can be used to produce low viscous coatings from Acrydur® 332, 418 and 510 in combination with mineral fillers and color pigments. The addition of Accelerator 440 shortens the curing time, resulting in a lower viscosity of the coating compound, which finally results in a good distribution at low soil temperatures. Acrydur® Accelerator 440 can be used as a binder for polymer concrete together with Hardener 10 PA.
 
Features:

	Property
	Measurement Method
	Approx. value

	Flashpoint
	DIN 51 755
	10 °C

	Density D²⁰
	DIN 51 757
	1 g/cm³

	Curing
	10-20 min. (20°C and 2% hardener) 

	Form of Delivery
	slightly cloudy liquid

	Shelf-life
	dark at < 20°C, 6 months maximum 

	Bundle
	25 kg, 10 kg Pails




Suggested formulation for Acrydur®
418 resin:	Acrydur® 440 is being used together with the coating compound directly on site.
.


Coating:	
Smooth-troweled	
	approx.- indications:

	20,0 weight parts Acrydur® 418

	2,0 weight parts Acrydur® Accelerator 440

	60,0 weight parts colored sand or quartz sand 0,7 – 1,2 mm

	18,0 weight parts colored sand or quartz sand 0,1 – 0,4 mm



Attention! The amount of resin can vary depending on the application. We therefore recommend that you test the resin content yourself! 
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Mix Acrydur® 440 and the coating resin Acrydur® 418 for approx. 1 minute in a suitable vessel. Add 1-3% hardener powder BPO 50%. Add dry filler to the prepared resin mixture and homogenize for 2 minutes. Apply to the surface primed with Acrydur® 112 using a squeegee and smoothing trowel.




Pot-and curing times depending on
the temperature:	
	Temperatur   [°C]
	Hardener  [Vol%]
	Hardener  [wt%]
	Pot life 
 [min]
	Curing time 
 [min]

	+ 5
	2.6
	4.0
	ca. 10
	ca. 30

	+ 10
	2.0
	3.0
	ca. 15
	ca. 25

	+ 20
	1.3
	2.0
	ca. 7
	ca. 20

	+ 30
	1.0
	1.5
	ca. 4
	ca. 18


                                        ● Hardener quantity is calculated on the net quantity of the resin component!



Notes:	Do not proceed until the previous coat is completely cured!



Storage:	Methacrylate resins are subject to the handling regulations of highly flammable materials. Acrydur® resins must be stored cool, at temperatures between 15 – 20° C and protected from direct sunlight. Paraffin particles may be deposited during storage. Therefore, materials must be stirred thoroughly before processing.
	Please follow the instructions in our Safety Data Sheet.



Processing:	When working with MMA resins, be sure to follow the safety precautions outlined in the Dangerous Goods Regulations!







Industrial safety: 

Provide adequate ventilation during work. During processing, observe the regulations of the Hazardous Substances Ordinance, the instructions of the Federal State Committee for Occupational Safety and Safety Technology (LASI), and our safety data sheets.





VbF: 			A I 

GISCODE: 		RMA 10 

HS-Code:	 	3208 2010
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	EN 13813, SR-B2, 0-AR0, 5-IR12

	Acrydur Accelerator® 440

	Synthetic resins for internal uses                                                                                                                                                                                                      (Application in accordance with the newest technical information)

	Reaction to fire:
	Efl

	Wear resistance (Abrasion Resistance):
	AR 0.5

	Impact resistance:
	IR 12

	Tensile bond strength:
	B 2.0


CE-labelling




data concerning our products and devices as well as concerning our data and procedures are based on an extensive research work and an application technology experience. We obtain these results, with which we do not take over adhesion going beyond the respective single contract, in word and writing after best knowledge, reserve ourselves we however technical changes in the course of the product development. Beyond that our application technology service stands when desired for large consultation as well as for co-operation
with the solution manufacturing and application technology problems for order. That does not relieve the user however to examine our data and recommendations before their use responsible for the own use. That applies - particularly for deliveries to foreign markets - also regarding the keeping of patent rights third as well as for applications and procedures, which are not expressly in writing indicated by us. The case of loss our adhesion is limited to indemnifications of same extent, as they plan our general terms of delivery and sales with lack of quality.
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