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Additive for Acrydur® Coatings

	

Application:	Adhesive Agent HP, in combination with our Acrydur® coating resins, enables coating on hot-dip galvanized and bare metal surfaces and serves as an adhesion primer for ceramic tiles.

Characteristics:	Adhesive Agent HP improves adhesion to metallic and ceramic substrates. Due to its highly corrosive properties, Adhesive Agent HP should be stored in its original container and mixed into the Acrydur® resins only immediately prior to application. Acrydur® resins containing Adhesive Agent HP are not shelf-stable!
 
Characteristics of the delivered product:

	Characteristic
	Measurement method
	Approximate value

	Density  D²⁰
	DIN EN ISO 1183-1
	 1,21g/cm³

	Flash point
	+10 °C

	Storage
	only in glass or polyethylene bottles

	Form of delivery
	Liquid, strongly acidic

	Shelf life
	In the dark at < 20 °C: maximum 6 months.

	Delivery Container
	                                25 kg Bucket ,
1 kg, 5 kg   Canister













________________________________________________________________________

Additional quantity:  0.2 to 0.3 wt.% (based on pure Acrydur® resin).

Standard Formulations:

1. Coating on sheet iron (degreased, blasted): approx. 1–2 mm

	100,0 GT
	Acrydur® 332

	0,2 GT	
	Adhesive Agent HP

	3,0 GT
	Hardener Powder 50 W (BPO 50%)


 




Broadcast the surface with corundum or quartz sand (0.5 – 1.0 mm).

	Pot life   (20 °C)
	                            approx. 20 min

	Time of Hardship (20 °C
	approx. 60 min.






Equally good adhesion is also achieved on other metals, such as aluminum. Achieved with copper and galvanized iron.

2. Coating of ceramic tiles. Prime using the following formulations:

	100,0 GT
	Acrydur® 118

	0,2 GT	
	Adhesive Agent HP

	4,0 GT
	Hardener Powder 50 W (BPO 50%)





                               

	Pot life  (20 °C)
	approx.. 10 min

	Time of Hardship (20 °C
	approx.. 35 min.





      
___________________Oder_________________________________________________

	100,0 GT
	Acrydur® 118

	0,5 GT	
	Adhesive Agent HP

	0,3 GT
	Accelerator B 101

	4,0 GT
	Hardener Powder 50 W (BPO 50%)









	Pot life   (20 °C)
	approx. 10 min

	Time of Hardship (20 °C
	approx. 40 min.






After this layer has cured, any desired topcoat—e.g., using Acrydur® 332 or Acrydur® 418—can be applied..


Notes:	The addition of Adhesive Agent HP to Acrydur® resins results in a delayed curing time and a more pronounced yellowing of the products. We therefore recommend that, in cases involving higher additions of Adhesive Agent HP (> 0.5%) or temperatures below 20 °C, an additional 0.2 to 0.3% of Accelerator 101 be added, and that the hardener content also be increased to 3–4%.

 Occupational 
Safety:	Ensure adequate ventilation during processing. The regulations of the LASI (State Committee for Occupational Safety) must be observed. Please read and follow the instructions provided in our safety data sheets.










VbF :		A I


HS-Code:		3824 9992
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	EN 13813, SR-B2, 0-AR0, 5-IR12

	Acrydur® Adhesive Agent HP HP  

	Application in accordance with the latest technical information  






CE- Labeling 

































Our information regarding our products, equipment, systems, and processes is based on extensive development work and practical application experience. We provide these findings—for which we assume no liability extending beyond the scope of the respective individual contract—both verbally and in writing to the best of our knowledge; however, we reserve the right to make technical modifications in the course of product development. Nevertheless, this does not absolve the user of the responsibility to independently verify the suitability of our products and processes for their own specific application. This also applies with regard to the observance of third-party intellectual property rights, as well as to applications and procedures that have not been expressly authorized by us in writing.
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